## Slide 1: DEVELOPMENT OF HIGH PERFORMANCE CONCRETE BY USING GRAPHENE OXIDE
PROJECT WORK GUIDED BY : PRESENTED BY :
MR.A. NAVEEN ARASU LIYA. T (720418103005)
ASSISTANT PROFESSOR RESHMI ABHAY (720418103006)
DEPARTMENT OF CIVIL ENGINEERING SAURAV SANTHOSH .K (720418103007)
CMS COLLEGE OF ENGINEERING
A TECHNOLOGY

## Slide 2: Presentation Outline
Abstract
Introduction
Objective
Literature Review
Methodology
Experimental Studies
Research gap
Expected outcome
Reference

## Slide 3: Abstract
The advancement of nano engineering technology plays a major role in the cementitious materials especially Graphene oxide which got the attention of many researchers. By the inclusion of Graphine oxide not only the strength but more durable and high resistance to water. Yet perhaps more importantly by including Graphine oxide we can reduce the amount of material required to make concrete. In this research the addition of Graphene Oxide in cement will be investigated for mechanical properties of concrete which is the macro level (workability, strength behavior, flexural behavior, water absorption, porosity, and durability) and micro level structural analysis (SEM analysis).

## Slide 4: Abstract (Cont….)
Normally the Graphene oxide is available in the powder form and it should be mixed with water to form a paste before mixing with concrete for better results. In this research varying percentages from 0 % to 2 % of GO is used to find the optimum percentage of GO by weight of ordinary Portland cement to obtain high strength. In this research Polycorboxylate ethers is planned to be used as super plasticizer.

## Slide 5: Introduction
Graphene oxide has a property of expanding in cold conditions and contract in hot conditions which will reduce the expansion and contraction cracks in concrete. The challenges to the application of cement like low fracture toughness, vulnerability to harmful penetration, low tensile strength can be reduced to a great extent. Graphene was manufactured by physical method and its purity exceeded 95%. The graphene consisted of 1–5 layers averaging 1.0–1.77 nm in thickness and 2–10 nm in diameter. Its specific surface ratio ranged from 360 to 450 m2/g.

## Slide 6: Introduction (Cont….)
There is an increase in 146% in compressive strength and 79.5% in flexural strength and decrease of about 400% in permeability compared to conventional concrete. Therefore it reduce the size of the structural components there by there will be a reduction of cost in construction.

## Slide 7: Objective
To increase mechanical properties of concrete (workability, strength behavior, flexural behavior, water absorption, porosity, and durability) and micro level structural analysis (SEM analysis) will be done.
Development of high performance concrete by using Graphene oxide.
To reduce drying shrinkage cracks.

## Slide 8: Literature Review
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
1 | Influence of graphene oxide on the mechanical properties, fracture toughness, and micro hardness of recycled concrete | Jianlin Luo , Shuaichao Chen , Qiuyi Li , Chao Liu , Song Gao, Jigang Zhang | Nanomaterials | MDPI | 2019 | XRD and SEM images demonstrate that GO incorporation can only improve the overlapping pattern and size regular morphology of hydration products rather than introduce new crystal phases into cementitious matrix
Notes: CNT – Carbon nanotube

## Slide 9
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
2 | Effect Of On Graphene Oxide the Concrete Resistance to Chloride Ion Permeability | Yihong Xu,Yingfang Fan | ACMME 2018 | IOP | 2018 | When the content of graphite oxide is low ,the resistance to chloride ion erosion is weaker than that of ordinary concrete , and the effect is the best when the content of graphite oxide is 0.03 of cement mass.

## Slide 10
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
3 | Review on the research progress of cement – based and geopolymer materials modified by graphene and graphene oxide | Changjiang Liu,Ziaochuan huang,Yu-You Wu,David Hui | Nanotechnology | DE GRUYTER | 2020 | The improvement effect of graphene based nanomaterials in geopolymers is also surprising providing a basis for expanding the application of geopolymers and also providing guidance and referance for the research of other types of geopolymer materials

## Slide 11
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
4 | Physical properties of concrete containing graphene oxide nano sheets | Yu-You Wu, Longxin Que, Zhaoyang Cui and Paul lambert | Materials | MDPI | 2019 | The slump of concrete containing GO nanosheets decreases with the addition of GO nanosheets from 0.02% to 0.80% by weight of cement under a water to cement ratio of 0.5 .

## Slide 12
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
5 | Effect of Graphene Oxide /Graphene Hybrid on Mechanical Properties of Cement Mortar and Mechanism Investigation | Hongfang Sun,Li Ling,Zhili Ren,Shazim Ali Memon, and Feng Xing | Nano materials | MDPI | January 2020 | The enhancement of flexural strength is related to the amount of GR addition and its dispersion in GO.Therefore it is believed that mechanical properties of mortar could be further increased if a more effective dispersant for GR can be found and used

## Slide 13
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
6 | Mechanical properties and shrinkage behaviour of concrete containing graphene-oxide nanosheets | Zengshun Chen,Yemeng Xu,Jiamin Hua,Xu Wang | materials | MDPI | 2020 | GO Nanosheets can considerbly improve the compressive strength at the age of 3,7 and 28 days.The higher the GO dosage is , the more obvious the strength increase will be.

## Slide 14
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
7 | Study on modification mechanism of workability and mechanical properties for graphene oxide reinforced cement composite | Yuxia Suo, Rongxin Guo,Haiting Xia | Nanomaterials and nano tchnology | Suo et al. | 2020 | The fluidity of cement paste is very sensitive to GO concteration and W/C.The experimental results show a noticeable inverse correlation between the concentration GO and fluidity,and positive linear correlation between W/C and fluidity,except GO concentration is high (>=0.2wt%).

## Slide 15
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
8 | Flexural fatigue behaviour and damage evolution analysis of edge oxidised graphene oxide(EOGO)reinforced concrete composites | Byoung Hooi Cho,Boo Hyun Nam,Mohammed Khawaji | Cement and concretecomposites | ELSEVIER | 2021 | EOGO reinforced concrete exhibited enhanced static compressive and flexural strengths.In particular,the largest effect of EOGO was recorded on the flexural strength of SFRC improved by 12.7%.

## Slide 16
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
9 | Surface abrasion resistance of high volume fly ash concrete modified by graphene oxide: macro – and micro perspectives | Sen Du , Yan Jiang , Jing Zhong | Construction and building materials | ELSEVIER | 2020 | Admixing GO at small dosage 0.01 to 0.1 % by weight of binder can significantly enhance the compressive strength and surface abrasion resistance of HVFA concrete 60% cement replacement by class C fly ash.

## Slide 17
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
10 | Effect of graphene oxid on mechanical and durability performance of concrete | S.C. Devi , R.A. Khan | Building Engineering | ELSEVIER | 2020 | Inclusion of GO with different percentage content by weight of cement in developing a concrete,as reduce the workability and significantly enhanced the compressive strength(21-55%)tensile sterngth(16-38%)

## Slide 18
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
11 | Compressive strength and durability behaviour of graphene oxide reinforced concrete composites containing recycled concrete aggregate | Sanglakpam Chiranjiakumari Devi,Rizwan Ahmed Khan | Building Engineering | ELSEVIER | 2020 | The present study concludeed that the 100% of RCA replacement in concrete can be made possible with addition of meager amount of graphene oxide with thickness ranging from 1 to 3 nm.

## Slide 19
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
12 | Mechanical prooerties and shrinkage behaviour of concrete containing graphene oxide nanosheets | Zengshun Chen,Yemeng Xu,Jiamin Hua,Xu Wang | Materials | MDPI | 2020 | GO nanosheets can considerably improve the compressive strength at the age of 3,7 and 28 days. The higher the GO dosage is, the more obvious the strength icrease will be. GO nanosheets of different contents can increase the compressive strength of concrete at the age of 28 days by 4.04-12.65%.

## Slide 20
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
13 | Physical Properties of concrete containing Graphene Oxide Nanosheets | Yu-You Wu,Longxin Que,Zhayang Cui | Materials | MDPI | 2019 | The slump of concrete containing GO nanosheets decreases with the addition of GO nanosheets from 0.02% to 0.80% by weight of cement under a water cement ratio 0.5. However, the workability of concrete is effected by both the addivtive and the GNPs.

## Slide 21
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
14 | Effect of graphene oxide on mechanical properties and durability of ultra high performance concrete prepared from recycled sand | Hongyan Chu , Yu Zang , Fengjuan Wang | Nanomaterials | MDPI | 2020 | The porosity of the RS-UHPC ranged between 2.19% and 2.47% .Adding GO to the RS-UHPC reduced the porosity by 4.45%-11.34%. The most propable pore size of RS-UHPC was reduced with the GO addition

## Slide 22
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
15 | Effect of graphene oxide nanosheets on physical properties of ultra high performance concrete with high volume supplementary cementitious materials | Yu-You Wu , Jing Zhang | Materials | MDPI | 2020 | The mini slump flow of UHPC with high volume CEMs decreases when the content of GO nanosheets increases from 0.01% to 0.05% by weight of cement for a given water to binder ratio of 0.16.

## Slide 23
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
16 | Research progress on individual effect of graphene oxide in cement –based material and its synergristic effect with other nanomaterials | Changjing Liu,Fulian Chen,David Hua,Jingwei Yang | Nanomaterials | DE GRUYTER | 2021 | Due to alkaline environment and high concentration of calcium ion GO will agglomerate in the cement.The dispersion of the GO mainly includes physical dispersion and chemical modification.

## Slide 24
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
17 | Application of nanomaterials in ultra high performance concrete | Changjiang Liu,Xin He,David Hui | Nanotechnology reviews | DE GRUYTER | 2020 | When these nanomaterials were added to UHPC,the water absorption rate of large specific surface area and filling effect became the key factors affecting the fluidity of UHPC except that CNFs and CNTs had little affect on fluidity at low dosage.

## Slide 25
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
18 | Ultra-high-performance cementitious composites with enhanced mechanical and durability characteristics | Muhammed M.Sadiq , Praviz Soroushian , Martin G.Backer | SN Applied Sciences | Springer Nature | 2021 | Flexural strength and abrasion resistance of UHPCM were greatly increased ,by 30% and 45% respectively with incorporation of acid functionalized MWNTs at 0.03% by weight of cement.

## Slide 26
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
19 | A review on the properties, reinforcing effects, and commercialization of nanomaterials for cement- based materials | Zhifang Zhao, Tianqi Qi, Wei Zhou, David Hui, Cong Xiao | Nanotechnology Reviews | De Gruyter | 2020 | Nanomaterials utilized in cement-based materials possess high specific surface area, nano-level size, and pozzolanic activity, which in turn lead to the nucleation effect ,filling effect, and bridging effect. Thus nanomaterials with superior properties can engineer cement-based materials to improve their mechanical properties,durabilty and sustainability.

## Slide 27
S. No | Title | Author(s) | Journal | Publisher | Issue/ Vol | Findings
20 | Improved Synthesis of Graphene Oxide | Daniela C. Marcano , Dmitry V. Kosynklin, Jacob M. Berlin, Alexander Sinitskii | ARTICLE | ACSNANO | 2010 | The protocol for running the reaction does not involve a large exotherm and produces no toxic gas.Moreover , the improved method yields a higher fraction of well – oxidized hydrophilic carbon material.This IGO is more oxidized than HGO and slightly more oxidized than HGO+ .

## Slide 28
METHODOLOGY
MATERIALS USED
Cement
Portland Pozzolana Cement (53 grade) conforming to IS: 12269 -1987 and with the specific gravity 3.15 was used for casting all the specimens. Tests conducted on cement are fineness of cement by sieve analysis (using 90 µ sieve), specific gravity using Le-chatlier’s apparatus, initial setting time and final setting time using vicat apparatus
Property of Cement | Values
Fineness Of Cement | 7.5%
Grade Of Cement | 53
Specific Gravity | 3.15
Initial Setting time | 28 min
Final Setting Time | 600 min

## Slide 29
Fine aggregate
Clean and dry river sand available locally was used. Sand passing through IS 4.75 mm sieve and as per IS: 383-1970 was used for all the specimens. Test conducted on fine aggregate are specific gravity using pycnometer, fineness modulus by sieve analysis.
Properties | Values
Specific Gravity | 2.64
Fineness Modulus | 2. 25

## Slide 30
Coarse aggregate
Crushed granite aggregate with specific gravity of 2.6 and passing through 20 mm sieve and retained on 12.5 mm sieve and as given in IS: 383 - 1970 is used for all the specimens
Properties | Values
Specific Gravity | 2.60
Size Of Aggregates | 20 mm
Fineness Modulus | 5.96

## Slide 31
Water
Casting and curing of specimens were done with the potable water as per IS 456:2000.
S.NO | WATER | pH VALUE
1. | Sample 1 | 7
2. | Sample 2 | 7
3. | Sample 3 | 7

## Slide 32
MIX DESIGN FOR M 60 GRADE CONCRETE
Concrete mix design for M 60 grade concrete
Type of cement used OPC 53 grade cement conforming to IS 269.
Maximum normal size of aggregate : 20 mm
Exposure condition : Severe exposure condition as per table 3 Page 18 in IS 456:2000.
Workability : 120 mm (Slump)
Method of concrete placing : Pumping
Degree of supervision : Good.
Type of aggregate used : Crushed angular aggregate.
Maximum cement content : 450 kg / m^3.
Chemical admixture type : Super-plasticizer (Polycarboxylate ether based)

## Slide 33
Material Properties:
Specific gravity of cement : 3.15
Specific gravity of course aggregate : 2.74
Specific gravity of fine aggregate : 2.65
Specific gravity of flyash : 2.20
Specific gravity of silica fume : 2.20
Specific gravity of chemical admixture : 1.08
Specific gravity of GO : 2.267
Water absorption of course aggregate : 0.5 %
Water absorption of fine aggregate : 1 %
Moisture content of fine and course aggregate : Nil
Entrapped air in concrete = 0.5 %

## Slide 34
Target Strength:
As per IS 10262 : 2019 table 1 and 2 of page 3
f’ck = fck+1.65 S or
f’ck = fck + X
f’ck = fck+1.65 S
= 60 +1.65 × 6.0 = 69.9 N/mm2
f’ck = fck + 6.5 (The value of X for M 60 grade as per Table 1 is 6.5 N/mm2)
= 60 + 6.5 = 66.5 N/mm2
The higher value is to be adopted
Selection of water-cementious materials ratio:
From Table 8, the water-cementitious materials ratio required for the target strength of 69.9 N/mm2 is 0.29 for msa 20 mm. This is lower than the maximum value of 0.45.
0.29< 0.45, hence O.K.

## Slide 35
Selection of water content
From Table 7, water content for 20 mm aggregate
= 186 kg/m3 (for 50 mm slump without using superplasticiser).
Estimated water content for 120 mm slump
= 186 + (8.4/100) X 186
= 201.624 say 202 kg/m3
As superplasticizer (Polycarboxylate ether based) is used, the water content can be reduced by 30 percent. Hence, the reduced water content
= 202 × 0.70
= 141.4 kg/m3 say 141 kg/m3

## Slide 36
Calculation of cement content
Water–cement ratio = 0.29 Water content
= 141 kg/m3
Cement content = 141 / 0.29
= 486.2 say 486 kg/m3
The cementitious material content
= 486 × 1.10
= 534.6 say 535 kg/m3
Fly ash @ 15 percent by weight of cementitious material
= 535 × 15 percent
= 80.25 kg/m3
Silica fume content @ 5 percent by weight of revised cementitious material = 535 × 5 percent
= 26.75 kg/m3

## Slide 37
Graphene oxide content @ 0.5 percent by weight of revised cementitious material
= 535 × 0.5 percent
= 2.675 kg/m3
Cement content = 535 - 26.75 - 80.25 – 2.675
= 425.325 kg/m3
Revised w/cm = 141 / 535 = 0.264
Check for minimum cementitious materials content,
320 kg/m3 < 535 kg/m3 (425.325 kg/m3 OPC + 26.75 kg/m3 silica fume + 80.25 kg/m3 fly ash + 2.675 kg/m3)
Hence OK
Check for maximum cement(OPC) content,
450 kg/m3> 425.325 kg/m3.
Hence OK.

## Slide 38
Proportion of volume of coarse aggregate and fine aggregate content
From Table 10, volume of coarse aggregate corresponding to 20 mm size aggregate and fine aggregate grading Zone II = 0.66 per unit volume of total aggregate. This is valid for water-cementitious materials ratio of 0.30. As water-cementitious material ratio is actually 0.264, the ratio is taken as 0.667.
Volume of fine aggregate content
= 1 – 0.667
= 0.333 per unit volume of total aggregate
Mix calculations
    Total volume = 1 m3
    Volume of entrapped air = 0.005 m3 in wet concrete

## Slide 39
    Volume of cement = (Mass of cement / Specific gravity of cement) x 1 / 1000
    = (425.325 / 3.15) x 1 / 1000
    = 0.135 m3
    Volume of water = (Mass of water / Specific gravity of water) x 1 / 1000
    = (141 / 1) x 1 / 1000
    = 0.141 m3
    Volume of silica fume = (Mass of silica fume / Specific gravity of silica fume) x 1 / 1000 = (26.75 / 2.2) x 1 / 1000
    = 0.0122 m3

## Slide 40
    Volume of fly ash = (Mass of fly ash / Specific gravity of fly ash ) x 1 / 1000
    = (80.25 / 2.2) x 1 / 1000
    = 0.0365 m3
    Volume of chemical admixture (superplasticizer) (@ 0.5 percent by mass of cementitious material)
    = (Mass of admixture / Specific gravity of admixture ) x 1 / 1000
    = (535 x 0.5% / 1.08) x 1 / 1000
    = 0.0025 m3
    Volume of GO = (Mass of GO / Specific gravity of GO) x 1 / 1000 = (2.675 / 2.267) x 1 / 1000
    = 0.0012 m3

## Slide 41
    Volume of all in aggregate = [(1-0.005) – (0.136 + 0.141 + 0.012 2 + 0.036 5 + 0.0025 + 0.0012)]
= 0.6658 m3
Mass of coarse aggregate = h × Volume of coarse aggregate × Specific gravity of coarse aggregate × 1000
= 0.667 × 0.667 × 2.74 × 1000
= 1218.9 kg say 1219 kg
Mass of fine aggregate = h × volume of fine aggregate × Specific gravity of fine aggregate × 1000
= 0.667 × 0.333 × 2.65 × 1 000
= 588.59 kg say 589 kg

## Slide 42
DESCRIPTION | QUANTITY
Volume of cement | 0.135m^3
Volume of water | 0.141m^3
Volume of silica fume | 0.0122m^3
Volume of fly ash | 0.0365m^3
Volume of chemical admixture | 0.0025m^3
Volume of GO | 0.0012m^3
Volume of all in aggregate | 0.6658m^3
Mass of coarse aggregate | 1219 kg
Mass of fine aggregate | 589 kg
MIX CALCULATIONS

## Slide 43
MIX PROPORTION | SLUMP VALUE (mm) | COMPACTION FACTOR
Conventional | 55 | 0.9944
M1 | 52.8 | 0.9900
M2 | 51.7 | 0.9845
M3 | 50.6 | 0.9790
WORKABILITY TEST

## Slide 44
MIX PROPORTION | 7days N/mm^2 | 14 days N/mm^2 | 28 days N/mm^2
Conventional | 27.72 | 43.56 | 68.2
M1 | 28.38 | 44.055 | 71.88
M2 | 29.04 | 46.2 | 75.24
M3 | 28.82 | 48.76 | 74.36
COMPRESSIVE STRENGTH TEST

## Slide 45: THANK YOU